APPROVAL SHEET

MODEL NO.：  SMD1206 Series

CUSTOMER：

CUSTOMER'S APPROVAL： AUTHORIZED SIGNATURE/STAMP DATE

MANUFACTURER: The Fourth Industrial Zone,Luokeng Village, Xiaotie District, Xiaojinkou Town, Huizhou City, Guangdong Province, China Tel: 0752-7213069/7213070 Fax: 0752-7213065 Submitted by: Approved by: Date:

Performance Specification

| Model | Marking |  |  |  |  |  | Maximum |  | Resistance |  | 认证 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | V max | Imax | I hold | I trip | Pd | Time To Trip |  |  |  |  |
|  |  |  |  | @25°C | @25°C | Typ. | Current | Time | R i min | R1max | UL |
|  |  | (V dc) | (A) | (A) | (A) | (W) | (A) | (Sec) | () | () |  |
| SMD1206R005SF60V | RA | 60.0 | 10 | 0.05 | 0.15 | 0.4 | 0.25 | 1.50 | 3.600 | 50.000 |  |
| SMD1206R005SF | RA | 24.0 | 10 | 0.05 | 0.15 | 0.4 | 0.25 | 1.50 | 3.600 | 50.000 | √ |
| SMD1206R010SF60V | R1 | 60.0 | 10 | 0.10 | 0.25 | 0.4 | 0.50 | 1.00 | 1.600 | 15.000 |  |
| SMD1206R010SF | R1 | 24.0 | 10 | 0.10 | 0.25 | 0.4 | 0.50 | 1.00 | 1.600 | 15.000 | √ |
| SMD1206R012SF60V | R1 | 60.0 | 10 | 0.12 | 0.29 | 0.4 | 0.50 | 1.00 | 1.600 | 15.000 |  |
| SMD1206R012SF | R1 | 24.0 | 10 | 0.12 | 0.29 | 0.4 | 0.50 | 1.00 | 1.600 | 13.000 | √ |
| SMD1206R016SF33V | R2 | 33.0 | 10 | 0.16 | 0.37 | 0.4 | 1.00 | 0.30 | 1.000 | 6.000 |  |
| SMD1206R016SF | R2 | 24.0 | 10 | 0.16 | 0.37 | 0.4 | 1.00 | 0.30 | 1.000 | 6.000 | √ |
| SMD1206R016SF16V | R2 | 16.0 | 10 | 0.16 | 0.37 | 0.4 | 1.00 | 0.30 | 1.000 | 6.000 |  |
| SMD1206R020SF | R2 | 24.0 | 10 | 0.20 | 0.46 | 0.6 | 8.00 | 0.08 | 0.350 | 2.700 | √ |
| SMD1206R020SF30V | R2 | 30.0 | 10 | 0.20 | 0.46 | 0.6 | 8.00 | 0.08 | 0.350 | 2.700 |  |
| SMD1206R020SF48V | R2 | 48.0 | 10 | 0.20 | 0.46 | 0.6 | 8.00 | 0.08 | 0.350 | 2.700 |  |
| SMD1206R025SF16V | R2 | 16.0 | 10 | 0.25 | 0.50 | 0.6 | 8.00 | 0.08 | 0.350 | 2.500 |  |
| SMD1206R025SF | R2 | 24.0 | 10 | 0.25 | 0.50 | 0.6 | 8.00 | 0.08 | 0.350 | 2.500 | √ |
| SMD1206R025SF30V | R2 | 30.0 | 10 | 0.25 | 0.50 | 0.6 | 8.00 | 0.08 | 0.350 | 2.500 |  |
| SMD1206R025SF48V | R2 | 48.0 | 10 | 0.25 | 0.50 | 0.6 | 8.00 | 0.08 | 0.350 | 2.500 |  |
| SMD1206R035SF | R3 | 6.0 | 35 | 0.35 | 0.75 | 0.6 | 8.00 | 0.10 | 0.250 | 1.300 | √ |
| SMD1206R035SF16V | R3 | 16 | 35 | 0.35 | 0.75 | 0.6 | 8.00 | 0.10 | 0.250 | 1.300 |  |
| SMD1206R035SF30V | R3 | 30.0 | 35 | 0.35 | 0.75 | 0.6 | 8.00 | 0.10 | 0.250 | 1.300 |  |
| SMD1206R050SF | R5 | 6.0 | 35 | 0.50 | 1.00 | 0.6 | 8.00 | 0.10 | 0.150 | 0.700 | √ |
| SMD1206R050SF13.2V | R5 | 13.2 | 35 | 0.50 | 1.00 | 0.6 | 8.00 | 0.10 | 0.150 | 0.700 |  |
| SMD1206R050SF16V | R5 | 16.0 | 35 | 0.50 | 1.00 | 0.6 | 8.00 | 0.10 | 0.150 | 0.700 |  |
| SMD1206R050SF30V | R5 | 30.0 | 35 | 0.50 | 1.00 | 0.6 | 8.00 | 0.10 | 0.150 | 0.700 |  |
| SMD1206R050SF33V | R5 | 33.0 | 35 | 0.50 | 1.00 | 0.6 | 8.00 | 0.10 | 0.150 | 0.700 |  |
| SMD1206R075SF | R7 | 6.0 | 35 | 0.75 | 1.50 | 0.6 | 8.00 | 0.20 | 0.090 | 0.500 | √ |
| SMD1206R075SF16V | R7 | 16.0 | 35 | 0.75 | 1.50 | 0.6 | 8.00 | 0.20 | 0.090 | 0.500 |  |
| SMD1206R075SF24V | R7 | 16.0 | 35 | 0.75 | 1.50 | 0.6 | 8.00 | 0.20 | 0.090 | 0.500 |  |
| SMD1206R075SF30V | R7 | 30.0 | 35 | 0.75 | 1.50 | 0.6 | 8.00 | 0.20 | 0.090 | 0.500 |  |
| SMD1206R100SF | R0 | 6.0 | 35 | 1.00 | 1.80 | 0.6 | 8.00 | 0.30 | 0.050 | 0.270 | √ |
| SMD1206R100SF16V | R0 | 16.0 | 35 | 1.00 | 1.80 | 0.6 | 8.00 | 0.30 | 0.050 | 0.270 |  |
| SMD1206R100SF24V | R0 | 24.0 | 35 | 1.00 | 1.80 | 0.6 | 8.00 | 0.30 | 0.050 | 0.270 |  |
| SMD1206R100SF30V | R0 | 30.0 | 35 | 1.00 | 1.80 | 0.6 | 8.00 | 0.30 | 0.050 | 0.270 |  |
| SMD1206R110SF | R0 | 6.0 | 35 | 1.10 | 2.20 | 0.6 | 8.00 | 0.30 | 0.040 | 0.250 | √ |
| SMD1206R110SF16V | R0 | 16.0 | 35 | 1.10 | 2.20 | 0.6 | 8.00 | 0.30 | 0.040 | 0.250 |  |
| SMD1206R110SF24V | R0 | 24.0 | 35 | 1.10 | 2.20 | 0.6 | 8.00 | 0.30 | 0.040 | 0.250 |  |
| SMD1206R110SF30V | R0 | 30.0 | 35 | 1.10 | 2.20 | 0.6 | 8.00 | 0.30 | 0.040 | 0.250 |  |
| SMD1206R125SF | RC | 6.0 | 35 | 1.25 | 2.50 | 0.6 | 8.00 | 0.30 | 0.030 | 0.190 |  |
| SMD1206R125SF12V | RC | 12 | 35 | 1.25 | 2.50 | 0.6 | 8.00 | 0.30 | 0.030 | 0.190 |  |
| SMD1206R150SF | RX | 6.0 | 35 | 1.50 | 3.00 | 0.8 | 8.00 | 0.30 | 0.025 | 0.130 | √ |
| SMD1206R150SF13.2V | RX | 13.2 | 35 | 1.50 | 3.00 | 0.8 | 8.00 | 0.30 | 0.025 | 0.130 |  |
| SMD1206R150SF16V | RX | 16 | 35 | 1.50 | 3.00 | 0.8 | 8.00 | 0.30 | 0.025 | 0.130 |  |
| SMD1206R200SF | RY | 6.0 | 35 | 2.00 | 3.50 | 0.8 | 8.00 | 1.50 | 0.015 | 0.080 | √ |
| SMD1206R200SF12V | RY | 12.0 | 35 | 2.00 | 3.50 | 0.8 | 8.00 | 1.50 | 0.015 | 0.080 |  |
| SMD1206R200SF16V | RY | 16.0 | 35 | 2.00 | 3.50 | 0.8 | 8.00 | 1.50 | 0.015 | 0.100 |  |
| SMD1206R250SF | RZ | 6.0 | 35 | 2.50 | 5.00 | 0.8 | 8.00 | 2.00 | 0.010 | 0.060 |  |
| SMD1206R250SF12V | RZ | 12.0 | 35 | 2.50 | 5.00 | 0.8 | 8.00 | 2.00 | 0.010 | 0.060 |  |
| SMD1206R260SF | RZ | 6.0 | 35 | 2.60 | 5.20 | 0.8 | 8.00 | 2.00 | 0.010 | 0.060 |  |
| SMD1206R260SF12V | RZ | 12.0 | 35 | 2.60 | 5.20 | 0.8 | 8.00 | 2.00 | 0.010 | 0.060 |  |
| SMD1206R300SF | RU | 6.0 | 35 | 3.00 | 6.00 | 1.0 | 8.00 | 4.00 | 0.010 | 0.050 |  |
| SMD1206R350SF | R- | 6.0 | 35 | 3.50 | 7.00 | 1.2 | 10.0 | 5.00 | 0.005 | 0.040 |  |

V max  = Maximum operating voltage device can withstand without damage at rated current (Imax).

I max   = Maximum fault current device can withstand without damage at rated voltage (V max).

I hold   = Hold Current. Maximum current device will not trip in 25°C still air.

I trip    = Trip Current. Minimum current at which the device will always trip in 25°C still air.

Pd      = Power dissipation when device is in the tripped state in 25°C still air environment at rated voltage.

Ri min/max  = Minimum/Maximum device resistance prior to tripping at 25°C.

R1max  = Maximum device resistance is measured one hour post reflow.

CAUTION : Operation beyond the specified ratings may result in damage and possible arcing and flame.

Environmental Specifications

| Test |  |  |  | Conditions |  |  |  | Resistance change |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Passive aging |  |  |  | +85°C, 1000 hrs. |  |  |  | I HOLD/I TRIP PASS |  |  |
| Humidity aging |  |  |  | +85°C, 85% R.H. , 168 hours |  |  |  | I HOLD/I TRIP PASS |  |  |
| Thermal shock |  |  |  | +85°C to -40°C, 20 times |  |  |  | I HOLD/I TRIP PASS |  |  |
| Resistance to solvent |  |  |  | MIL-STD-202,Method 215 |  |  |  | No change |  |  |
| Vibration |  |  |  | MIL-STD-202,Method 201 |  |  |  | No change |  |  |
| Ambient operating conditions : - 40 °C to +85 °C |  |  |  |  |  |  |  |  |  |  |
| Maximum surface temperature of the device in the tripped state is 125 °C |  |  |  |  |  |  |  |  |  |  |

Agency Approval and Environmental Complianc

| Agency | File Number |  | Regulation | Standard |
| --- | --- | --- | --- | --- |
| UL | E486890 |  |  | 2002/95/EC |
| TUV | pending |  |  | EN14582 |

Thermal Derading Chart

Recommended Hold Current(A) at Ambient Temperature(°C)

| Model | Ambient Operation Temperature |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | -40°C | -20°C | 0°C | 25°C | 40°C | 50°C | 60°C | 70°C | 85°C |
| SMD1206R005SF | 0.074 | 0.066 | 0.058 | 0.05 | 0.0425 | 0.0375 | 0.035 | 0.03 | 0.0275 |
| SMD1206R010SF | 0.148 | 0.132 | 0.116 | 0.10 | 0.085 | 0.075 | 0.07 | 0.06 | 0.055 |
| SMD1206R012SF | 0.18 | 0.16 | 0.14 | 0.12 | 0.10 | 0.09 | 0.08 | 0.07 | 0.07 |
| SMD1206R016SF | 0.24 | 0.21 | 0.18 | 0.16 | 0.14 | 0.13 | 0.12 | 0.11 | 0.10 |
| SMD1206R020SF | 0.30 | 0.26 | 0.23 | 0.20 | 0.17 | 0.15 | 0.14 | 0.12 | 0.11 |
| SMD1206R025SF | 0.37 | 0.33 | 0.29 | 0.25 | 0.22 | 0.20 | 0.17 | 0.15 | 0.12 |
| SMD1206R035SF | 0.50 | 0.45 | 0.40 | 0.35 | 0.30 | 0.27 | 0.24 | 0.21 | 0.15 |
| SMD1206R050SF | 0.71 | 0.64 | 0.57 | 0.50 | 0.42 | 0.39 | 0.35 | 0.31 | 0.25 |
| SMD1206R075SF | 1.14 | 1.01 | 0.88 | 0.75 | 0.65 | 0.59 | 0.54 | 0.49 | 0.41 |
| SMD1206R100SF | 1.45 | 1.31 | 1.15 | 1.00 | 0.84 | 0.77 | 0.69 | 0.61 | 0.48 |
| SMD1206R110SF | 1.60 | 1.45 | 1.30 | 1.10 | 0.95 | 0.80 | 0.72 | 0.66 | 0.55 |
| SMD1206R125SF | 2.0 | 1.75 | 1.52 | 1.25 | 1.00 | 0.95 | 0.90 | 0.75 | 0.53 |
| SMD1206R150SF | 2.18 | 1.94 | 1.72 | 1.50 | 1.28 | 1.17 | 1.06 | 0.96 | 0.77 |
| SMD1206R200SF | 2.88 | 2.63 | 2.34 | 2.00 | 1.74 | 1.58 | 1.42 | 1.17 | 0.93 |
| SMD1206R250SF | 3.30 | 3.10 | 2.82 | 2.50 | 2.16 | 1.98 | 1.83 | 1.54 | 1.33 |
| SMD1206R260SF | 3.43 | 3.22 | 2.93 | 2.60 | 2.23 | 2.03 | 1.87 | 1.57 | 1.35 |
| SMD1206R300SF | 4.05 | 3.66 | 3.36 | 3.00 | 2.50 | 2.28 | 2.00 | 1.62 | 1.35 |
| SMD1206R350SF | 4.65 | 4.23 | 3.92 | 3.50 | 2.92 | 2.68 | 2.35 | 1.91 | 1.42 |

Thermal Derating Curve              Average Time-Current Curve

Soldering Parameters

t L

60~150 s

ts

Preheat 60~180 s

t 25°C to peak

Time

Temperature(°C)

TL 217

TP 260

25

TP 20~40 S

Ramp-up

Critical Zone

TL to TP

Ramp-down

Tsmax

Tsmin

150

200

| Profile Feature | Pb-Free Assembly |
| --- | --- |
| Average Ramp-Up Rate(Ts max to T p) | 3℃/second mac. |
| Preheat -Temperature Min(Ts min) -Temperature Max(Ts max) -Time(Ts min to Ts max) | 150℃ 200℃ 60~180 seconds |
| Time maintained above: -Temperature(TL) -Time(tL) | 217℃ 60~150 seconds |
| Peak Temperature(Tp) | 260℃ |
| Ramp-Down Rate | 6℃/second max. |
| Time 25℃ to Peak Temperature | 8 minutes max |
| Storage Condition | 遮光密封 |

Recommended reflow methods: IR, vapor phase oven, hot air oven, N2 environment for lead-free

Recommended maximum paste thickness is 0.25mm

Devices can be cleaned using standard industry methods and solvents.

Note 1:All temperature refer to topside of the package, measured on the package body surface.

Note 2: If reflow temperatures exceed the recommended profile, devices may not meet the performance requirements.

Physical Dimensions(mm.)

C

E

B

A

D

3

| Model | A |  | B |  | C |  | D | E |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Min. | Max. | Min. | Max. | Min. | Max. | Min. | Min. |
| SMD1206R005SF60V | 3.00 | 3.60 | 1.50 | 1.90 | 0.60 | 1.20 | 0.15 | 0.10 |
| SMD1206R005SF | 3.00 | 3.60 | 1.50 | 1.90 | 0.60 | 1.20 | 0.15 | 0.10 |
| SMD1206R010SF60V | 3.00 | 3.60 | 1.50 | 1.90 | 0.60 | 1.20 | 0.15 | 0.10 |
| SMD1206R010SF | 3.00 | 3.60 | 1.50 | 1.90 | 0.60 | 1.20 | 0.15 | 0.10 |
| SMD1206R012SF60V | 3.00 | 3.60 | 1.50 | 1.90 | 0.60 | 1.20 | 0.15 | 0.10 |
| SMD1206R012SF | 3.00 | 3.60 | 1.50 | 1.90 | 0.60 | 1.20 | 0.15 | 0.10 |
| SMD1206R016SF33V | 3.00 | 3.60 | 1.50 | 1.90 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD1206R016SF | 3.00 | 3.60 | 1.50 | 1.90 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD1206R016SF16V | 3.00 | 3.60 | 1.50 | 1.90 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD1206R020SF | 3.00 | 3.60 | 1.50 | 1.90 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD1206R020SF30V | 3.00 | 3.60 | 1.50 | 1.90 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD1206R020SF48V | 3.00 | 3.60 | 1.50 | 1.90 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD1206R025SF16V | 3.00 | 3.60 | 1.50 | 1.90 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD1206R025SF | 3.00 | 3.60 | 1.50 | 1.90 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD1206R025SF30V | 3.00 | 3.60 | 1.50 | 1.90 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD1206R025SF48V | 3.00 | 3.60 | 1.50 | 1.90 | 0.40 | 1.00 | 0.15 | 0.10 |
| SMD1206R035SF | 3.00 | 3.60 | 1.50 | 1.90 | 0.35 | 0.8 | 0.15 | 0.10 |
| SMD1206R035SF16V | 3.00 | 3.60 | 1.50 | 1.90 | 0.35 | 0.8 | 0.15 | 0.10 |
| SMD1206R035SF30V | 3.00 | 3.60 | 1.50 | 1.90 | 0.40 | 0.9 | 0.15 | 0.10 |
| SMD1206R050SF | 3.00 | 3.60 | 1.50 | 1.90 | 0.35 | 0.8 | 0.15 | 0.10 |
| SMD1206R050SF13.2V | 3.00 | 3.60 | 1.50 | 1.90 | 0.35 | 0.80 | 0.15 | 0.10 |
| SMD1206R050SF16V | 3.00 | 3.60 | 1.50 | 1.90 | 0.35 | 0.8 | 0.15 | 0.10 |
| SMD1206R050SF30V | 3.00 | 3.60 | 1.50 | 1.90 | 0.50 | 1.00 | 0.15 | 0.10 |
| SMD1206R050SF33V | 3.00 | 3.60 | 1.50 | 1.90 | 0.60 | 1.50 | 0.15 | 0.10 |
| SMD1206R075SF | 3.00 | 3.60 | 1.50 | 1.90 | 0.35 | 0.80 | 0.15 | 0.10 |
| SMD1206R075SF16V | 3.00 | 3.60 | 1.50 | 1.90 | 0.50 | 1.00 | 0.15 | 0.10 |
| SMD1206R075SF24V | 3.00 | 3.60 | 1.50 | 1.90 | 0.60 | 1.20 | 0.15 | 0.10 |
| SMD1206R075SF30V | 3.00 | 3.60 | 1.50 | 1.90 | 0.70 | 1.30 | 0.15 | 0.10 |
| SMD1206R100SF | 3.00 | 3.60 | 1.50 | 1.90 | 0.35 | 0.80 | 0.15 | 0.10 |
| SMD1206R100SF16V | 3.00 | 3.60 | 1.50 | 1.90 | 0.50 | 1.00 | 0.15 | 0.10 |
| SMD1206R100SF24V | 3.00 | 3.60 | 1.50 | 1.90 | 0.70 | 1.30 | 0.15 | 0.10 |
| SMD1206R100SF30V | 3.00 | 3.60 | 1.50 | 1.90 | 0.70 | 1.30 | 0.15 | 0.10 |
| SMD1206R110SF | 3.00 | 3.60 | 1.50 | 1.90 | 0.35 | 0.80 | 0.15 | 0.10 |
| SMD1206R110SF16V | 3.00 | 3.60 | 1.50 | 1.90 | 0.50 | 1.00 | 0.15 | 0.10 |
| SMD1206R110SF24V | 3.00 | 3.60 | 1.50 | 1.90 | 0.70 | 1.30 | 0.15 | 0.10 |
| SMD1206R110SF30V | 3.00 | 3.60 | 1.50 | 1.90 | 0.70 | 1.30 | 0.15 | 0.10 |
| SMD1206R125SF | 3.00 | 3.60 | 1.50 | 1.90 | 0.50 | 1.10 | 0.15 | 0.10 |
| SMD1206R125SF12V | 3.00 | 3.60 | 1.50 | 1.90 | 0.50 | 1.10 | 0.15 | 0.10 |
| SMD1206R150SF | 3.00 | 3.60 | 1.50 | 1.90 | 0.50 | 1.00 | 0.15 | 0.10 |
| SMD1206R150SF13.2V | 3.00 | 3.60 | 1.50 | 1.90 | 1.00 | 1.60 | 0.15 | 0.10 |
| SMD1206R150SF16V | 3.00 | 3.60 | 1.50 | 1.90 | 1.00 | 1.60 | 0.15 | 0.10 |
| SMD1206R200SF | 3.00 | 3.60 | 1.50 | 1.90 | 0.7 | 1.30 | 0.15 | 0.10 |
| SMD1206R200SF12V | 3.00 | 3.60 | 1.50 | 1.90 | 1.00 | 1.60 | 0.15 | 0.10 |
| SMD1206R200SF16V | 3.00 | 3.60 | 1.50 | 1.90 | 1.00 | 1.60 | 0.15 | 0.10 |
| SMD1206R250SF | 3.00 | 3.60 | 1.50 | 1.90 | 1.00 | 1.60 | 0.15 | 0.10 |
| SMD1206R250SF12V | 3.00 | 3.60 | 1.50 | 1.90 | 1.00 | 1.60 | 0.15 | 0.10 |
| SMD1206R260SF | 3.00 | 3.60 | 1.50 | 1.90 | 1.00 | 1.60 | 0.15 | 0.10 |
| SMD1206R260SF 12V | 3.00 | 3.60 | 1.50 | 1.90 | 1.00 | 1.60 | 0.15 | 0.10 |
| SMD1206R300SF | 3.00 | 3.60 | 1.50 | 1.90 | 1.00 | 1.60 | 0.15 | 0.10 |
| SMD1206R350SF | 3.00 | 3.60 | 1.50 | 1.90 | 1.00 | 1.60 | 0.15 | 0.10 |

Termination Pad Characteristics

Terminal pad materials：Tin-plated Nickel-Copper

Terminal pad solder ability：Meets EIA specification RS186-9E and ANSI/J-STD-002 Category 3.

Recommended Pad Layout (mm.)

1.9士0.1

1.0士0.1

1.0 士0.1

1.9士0.1

注：在此印锡面积条件下，推荐钢网厚度为≧0.12MM(钢网厚度不够要增大刷锡面积）

Packaging Quantity

| Part Number | Quantity | Part Number | Quantity |
| --- | --- | --- | --- |
| SMD1206R005.010.012SF | 3500 pcs/reel | SMD1206R100SF | 4500 pcs/reel |
| SMD1206R016.020.025SF | 4500 pcs/reel | SMD1206R100SF16V~30V | 3500 pcs/reel |
| SMD1206R035SF | 4500 pcs/reel | SMD1206R110SF | 4500 pcs/reel |
| SMD1206R035SF16V | 4500 pcs/reel | SMD1206R110SF16V~30V | 3500 pcs/reel |
| SMD1206R035SF24V~30V | 3500 pcs/reel | SMD1206R125SF | 4500 pcs/reel |
| SMD1206R050SF | 4500 pcs/reel | SMD1206R125SF16V | 3500 pcs/reel |
| SMD1206R050SF13.2V~33V | 3500 pcs/reel | SMD1206R150.200.250.260SF | 3500 pcs/reel |
| SMD1206R075SF | 4500 pcs/reel | SMD1206R300.350SF | 3500 pcs/reel |
| SMD1206R075SF16V~30V | 3500 pcs/reel |  |  |

Tape & reel packaging per EIA481-1

Tape And Reel Specifications (mm)

P1

W

E2

F

E1

P0

P2

B0

K0

B1

T1

Cover tape

D0

A0

Embossment

T

EIA Tape Component Dimensions

| Governing Specifications |  | EIA 481-1 |
| --- | --- | --- |
| W |  | 8.15 ± 0.3 |
| P0 |  | 4.0 ± 0.10 |
| P1 |  | 4.0 ± 0.10 |
| P2 |  | 2.0 ± 0.05 |
| A0 |  | 1.95 ± 0.10 |
| B0 |  | 3.40 ± 0.10 |
| B1max. |  | 4.35 |
| D0 |  | 1.50 + 0.1, -0 |
| F |  | 3.5 ± 0.05 |
| E1 |  | 1.75 ± 0.10 |
| E2min. |  | 6.25 |
| T |  | 0.6 |
| T1max. |  | 0.1 |
| K0 |  | 1.04 ± 0.1 |
| Leader min. |  | 390 |
| Trailer min. |  | 160 |
| Reel Dimensions |  |  |
| A max. |  | 178 |
| N min. |  | 60 |
| W1 |  | 9 ± 0.5 |
| W2 |  | 12.6 ± 0.5 |
| Storage And Handling |  |  |
| ‧ Storage conditions：遮光密封 |  |  |
| ‧ Devices may not meet specified performance |  |  |
| if storage conditions are exceeded. |  |  |

Embossed cavity

Cover tape

Carrier tape

A

W2(measured at hub)

N(hub dia.)

W1(measured at hub)

2

2

2

0

EIA Reel Dimensions

Part Number System

SMD 1206 R 口口口 S F 口口V
                                           special voltage Rating(Optional)

Lead-Free

Tin-plated Nickel-Copper

Holding Current Rating

Da Rong

Device Dimensions: Length/width(Unit:1/100 inch) Size 3216 mm / 1206 inch

Surface Mount Device

注意事项

PPTC使用注意事项：

·PPTC为热敏元件，对环境温度比较敏感，建议在PPTC周围不要设计热源元件，环境温度最高控制在85℃以下，尽量减少外部热源的影响，否则会影响产品性能导致焊后电阻大于规格。

·请在规格书规定的参数下(<10%)使用，超出电压电流规格值，会导致PPTC出现电弧，阻值升高，甚至烧片。

·规格书的电气特性，均是基于在大容指定测试板经过一次回流焊之后的测试；如果客户有二次回流焊或者注塑点胶等其他热工序，会对上述参数有一定程度的衰减，需要验证其适用性。

. PPTC设备在故障状态下会发生热膨胀。如果PPTC装置安装或放置在PPTC装置与周围材料（如覆盖材料、包装材料、封装材料等）之间的空间不足的应用中，将对热膨胀产生抑制作用。挤压、扭曲、弯曲和其他类型的机械应力也会对PPTC设备的性能产生不利影响，不得使用或施加。

·PPTC贴片产品是为SMT工艺设计的封装形式，焊接工艺为回流焊；要求客户遵守我们推荐的焊盘布局和回流焊配置文件。不正确的电路板布局或回流配置可能会对PPTC的可焊性性能产生负面影响。焊接工艺可参考大容推荐的回流焊曲线。如果回流焊温度超过推荐的值，PPTC将有可能受到损伤。使用手工焊及波峰焊接PPTC可能会导致产品焊后电阻超出规格。

·某些注塑料、单组份、双组份固化胶粘剂、硅胶、特种润滑理基脂、侵蚀性溶剂、石蜡污染PPTC材料破坏芯片，需要对注塑料胶料、石蜡等材料牌号以及应用参数（如温度、时间等）进行验证，以确保产品及工艺的匹配性，确认不会影响PPTC性能之后方可使用。PPTC在充电线端应用中，建议使用PP类材料做内膜，禁止使用TPE类与PVC类等材料做内膜。

·PPTC贴装或使用过程中，不建议使用洗板水或其他清洗剂进行清洗。如必须使用，需要验证各类清洗剂、洗板水以及溶剂的适用性，确认不会影响PPTC性能之后方可使用。已知对PPTC有影响的化学药品包括但不仅限于醚类、苯类、酮类以及脂类等较强溶解性、破坏性的有机化合物，清洗后将产品放置于敞开的环境中至少24小时，将残留的溶剂进行充分的挥发。

·装配过程中，避免用暴力砸、挤、压、拉、扭、刺等方式作用PPTC本体，以免引起PPTC 性能衰减。

·PPTC元件是为电路中偶尔出现的过流而设计的，不建议用在连续且持续过流、重复故障的电路中（此类故障情况可能是由连接器的错误引脚连接引起的），或过大范围跳闸事件可能发生时，不得使用。

·大容SMD PPTC产品为遮光密封包装。客户如在库存中发现有包装破损的，立即将产品隔离处理；使用时如有余料，需恢复之前包装状态，做遮光密封保存，否则会影响产品性能导致焊后电阻大于规格。

·产品废弃时，可按照一般电子废弃物处理，具体材料组成可参见MSDS

如果以上注意事项的任何项目未得到遵守，则免除所有的责任。